Supplementary Material: Predictive Multi-Physics Modelling of Al-Zn-Mg-Sn Sacrificial Anodes: A Data-Driven Microstructure-to-Performance Framework for Sustainable Cathodic Protection

Table of Contents

- Parameter Estimation Results

- Bootstrap Uncertainty Analysis

- Covariance Matrix

- Cross-Validation Results

- Computational Implementation Details

S1. Parameter Estimation Results {#parameter-estimation}

Table S1. Fitted Model Parameters with Standard Errors

| Parameter | Symbol | Value | Std Error | 95% CI Lower | 95% CI Upper | Unit | CV (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Baseline exchange current | i₀,base | 1.584 | 0.082 | 1.423 | 1.745 | mA/cm² | 5.2 |
| Precipitation rate constant | k₀ | 4.82×10⁻⁵ | 3.1×10⁻⁶ | 4.21×10⁻⁵ | 5.43×10⁻⁵ | s⁻¹ | 6.4 |
| Precipitation coupling | β | 2.145 | 0.156 | 1.839 | 2.451 | - | 7.3 |
| Compositional sensitivity | γ | 8.762 | 0.623 | 7.541 | 9.983 | wt%⁻¹ | 7.1 |

Notes:

- Standard errors calculated from asymptotic covariance matrix

- 95% confidence intervals based on normal approximation (t-distribution for n=280)

- CV = Coefficient of variation (Std Error / Value × 100%)

- All parameters statistically significant (p < 0.001)

Table S2. Fixed Model Parameters (Literature Values)

| Parameter | Symbol | Value | Unit | Source |
| --- | --- | --- | --- | --- |
| Activation energy | Q | 125 | kJ/mol | Feng et al. (2022) [29] |
| Avrami exponent | n | 2.0 | - | DSC analysis [29] |
| Power-law exponent | m | 0.68 | - | Calibrated to microstructure data |
| Anodic transfer coefficient | αₐ | 0.5 | - | Standard for Al dissolution [21] |
| Temperature | T | 25 | °C | Seawater immersion conditions |
| Anode efficiency | η | 90 | % | Typical for Al-Zn alloys [1,2] |

S2. Bootstrap Uncertainty Analysis {#bootstrap-analysis}

Table S3. Bootstrap Parameter Distributions (n = 1000 iterations)

| Parameter | Mean | Median | Std Dev | CV (%) | 90% CI Lower | 90% CI Upper | 95% CI Lower | 95% CI Upper |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| i₀,base (mA/cm²) | 1.591 | 1.586 | 0.089 | 5.6 | 1.444 | 1.745 | 1.418 | 1.771 |
| k₀ (×10⁻⁵ s⁻¹) | 4.85 | 4.81 | 0.34 | 7.0 | 4.29 | 5.47 | 4.18 | 5.56 |
| β | 2.158 | 2.142 | 0.168 | 7.8 | 1.881 | 2.456 | 1.835 | 2.503 |
| γ (wt%⁻¹) | 8.801 | 8.745 | 0.671 | 7.6 | 7.693 | 9.921 | 7.559 | 10.115 |

Bootstrap Statistics:

- Number of bootstrap samples: 1000

- Successful convergence rate: 94.3% (943/1000)

- Bootstrap method: Nonparametric resampling with replacement

- Confidence intervals: Percentile method

- Mean R² across bootstrap samples: 0.884 ± 0.018

- Mean RMSE across bootstrap samples: 0.289 ± 0.025 mA/cm²

Table S4. Parameter Significance Assessment

| Parameter | t-statistic | p-value | Significance | Physical Interpretation |
| --- | --- | --- | --- | --- |
| i₀,base | 19.3 | <0.001 | *** | Highly significant baseline activity |
| k₀ | 15.5 | <0.001 | *** | Precipitation kinetics well-constrained |
| β | 13.8 | <0.001 | *** | Strong precipitation-electrochemistry coupling |
| γ | 14.1 | <0.001 | *** | Significant compositional effect of Sn |

Significance codes: *** p < 0.001, ** p < 0.01, * p < 0.05

S3. Covariance and Correlation Matrices {#covariance-matrix}

Table S5. Parameter Covariance Matrix

|  | i₀,base | k₀ | β | γ |
| --- | --- | --- | --- | --- |
| i₀,base | 6.72×10⁻³ | -2.18×10⁻⁷ | 1.05×10⁻² | 3.92×10⁻² |
| k₀ | -2.18×10⁻⁷ | 9.61×10⁻¹² | -3.87×10⁻⁷ | -1.45×10⁻⁶ |
| β | 1.05×10⁻² | -3.87×10⁻⁷ | 2.43×10⁻² | 7.28×10⁻² |
| γ | 3.92×10⁻² | -1.45×10⁻⁶ | 7.28×10⁻² | 3.88×10⁻¹ |

Table S6. Parameter Correlation Matrix

|  | i₀,base | k₀ | β | γ |
| --- | --- | --- | --- | --- |
| i₀,base | 1.000 | -0.271 | 0.821 | 0.767 |
| k₀ | -0.271 | 1.000 | -0.253 | -0.237 |
| β | 0.821 | -0.253 | 1.000 | 0.750 |
| γ | 0.767 | -0.237 | 0.750 | 1.000 |

Interpretation:

- Strong positive correlation between i₀,base and β (r = 0.821): Higher baseline activity co-varies with stronger precipitation effects

- Strong positive correlation between β and γ (r = 0.750): Precipitation and compositional effects are coupled

- Moderate negative correlation between k₀ and other parameters: Faster precipitation kinetics associated with lower baseline activities

- All correlations statistically significant (p < 0.01)

S4. Cross-Validation Results {#cross-validation}

Table S7. Five-Fold Cross-Validation Performance

| Fold | Training R² | Validation R² | Training RMSE | Validation RMSE | MAPE (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 0.893 | 0.876 | 0.278 | 0.299 | 17.8 |
| 2 | 0.889 | 0.881 | 0.282 | 0.293 | 18.5 |
| 3 | 0.891 | 0.884 | 0.280 | 0.289 | 18.1 |
| 4 | 0.886 | 0.892 | 0.287 | 0.279 | 17.9 |
| 5 | 0.894 | 0.879 | 0.276 | 0.295 | 18.7 |
| Mean | 0.891 | 0.882 | 0.281 | 0.291 | 18.2 |
| Std Dev | 0.003 | 0.006 | 0.004 | 0.007 | 0.4 |

Validation Statistics:

- No evidence of overfitting (training and validation R² within 1%)

- Consistent performance across all folds (CV < 1% for R²)

- RMSE difference between training/validation: 3.6% (acceptable)

Table S8. Model Performance by Subset

| Subset | N | R² | RMSE (mA/cm²) | MAPE (%) | Max Residual |
| --- | --- | --- | --- | --- | --- |
| By Sn Composition |  |  |  |  |  |
| 0.00 wt% | 70 | 0.891 | 0.291 | 18.9 | 0.583 |
| 0.01 wt% | 70 | 0.884 | 0.273 | 17.2 | 0.547 |
| 0.05 wt% | 70 | 0.912 | 0.245 | 16.8 | 0.489 |
| 0.10 wt% | 70 | 0.823 | 0.318 | 20.3 | 0.641 |
| By Temperature |  |  |  |  |  |
| As-cast (25°C) | 28 | 0.891 | 0.291 | 18.9 | 0.583 |
| 130°C | 84 | 0.868 | 0.312 | 19.8 | 0.628 |
| 160°C | 84 | 0.898 | 0.267 | 17.3 | 0.534 |
| 190°C | 84 | 0.872 | 0.301 | 19.1 | 0.605 |
| By Aging Time |  |  |  |  |  |
| 0 h (as-cast) | 28 | 0.891 | 0.291 | 18.9 | 0.583 |
| 4 h | 84 | 0.903 | 0.258 | 16.7 | 0.516 |
| 8 h | 84 | 0.882 | 0.287 | 18.4 | 0.574 |
| 12 h | 84 | 0.874 | 0.294 | 19.2 | 0.589 |
| By Exposure Time |  |  |  |  |  |
| 48-96 h | 80 | 0.878 | 0.305 | 19.6 | 0.612 |
| 144-336 h | 200 | 0.892 | 0.268 | 17.5 | 0.537 |

Observations:

- Best performance at 0.05 wt% Sn (R² = 0.912): Optimal composition for model accuracy

- Slightly elevated scatter at 0.10 wt% Sn: Additional intermetallic phases not fully captured

- Temperature dependence well-captured: Consistent R² > 0.86 across all conditions

- Early-time slight bias: +0.021 mA/cm² mean residual at 48-96h vs -0.003 at 144-336h

S5. Computational Implementation Details {#implementation}

Table S9. Numerical Solver Configuration

| Parameter | Value | Description |
| --- | --- | --- |
| Optimization Algorithm |  |  |
| Method | Trust Region Reflective (TRF) | Handles bounded constraints efficiently |
| Max iterations | 500 | Typical convergence: 120-140 iterations |
| Function tolerance | 1×10⁻⁸ | Objective function convergence criterion |
| Parameter tolerance | 1×10⁻⁸ | Parameter change convergence criterion |
| Gradient tolerance | 1×10⁻⁸ | Gradient norm convergence criterion |
| Time Integration |  |  |
| Initial timestep | 60 s | Adaptive refinement enabled |
| Simulation horizon | 336 h | Laboratory exposure duration |
| Service life horizon | 15 years | Long-term prediction extrapolation |
| Convergence tolerance | 0.01% | Butler-Volmer iterative solver |
| Numerical Stability |  |  |
| Jacobian estimation | Forward differences | 2-point stencil |
| Condition number | < 1000 | Well-conditioned parameter space |
| Residual tolerance | 0.5% | Per-iteration convergence check |

Table S10. Computational Performance Metrics

| Task | Runtime | Memory Usage | Notes |
| --- | --- | --- | --- |
| Single prediction | 0.3 ms | 2 MB | Vectorized numpy operations |
| Full dataset (280 pts) | 84 ms | 12 MB | Batch processing |
| Parameter fitting | 3.2 s | 45 MB | 127 iterations to convergence |
| Bootstrap (1000 iter) | 53 min | 180 MB | Parallelizable (not implemented) |
| Service life simulation | 1.8 s | 25 MB | 1000 timesteps over 15 years |

Hardware Specifications:

- CPU: Intel Core i7-10700K @ 3.8 GHz

- RAM: 32 GB DDR4

- Python: 3.9.13

- NumPy: 1.23.5

- SciPy: 1.10.1

S6. Sensitivity Analysis Results

Table S11. Local Parameter Sensitivity

| Parameter | Nominal Value | ±10% Perturbation Effect on i_avg | Sensitivity Rank |
| --- | --- | --- | --- |
| γ (Sn sensitivity) | 8.762 wt%⁻¹ | ±18.7% | 1 (Highest) |
| β (precipitation coupling) | 2.145 | ±15.3% | 2 |
| i₀,base | 1.584 mA/cm² | ±10.0% | 3 |
| k₀ | 4.82×10⁻⁵ s⁻¹ | ±6.8% | 4 (Lowest) |

Interpretation:

- Compositional term (γ) has strongest influence on predictions

- Precipitation coupling (β) second most influential

- Rate constant (k₀) least sensitive: transformation kinetics well-constrained by time-temperature

- All parameters within acceptable sensitivity range (no excessive leverage)

Table S12. Global Sensitivity Analysis (Sobol Indices)

| Parameter | First-order Index | Total-order Index | Interaction Contribution |
| --- | --- | --- | --- |
| i₀,base | 0.24 | 0.38 | 0.14 |
| k₀ | 0.12 | 0.18 | 0.06 |
| β | 0.31 | 0.47 | 0.16 |
| γ | 0.33 | 0.52 | 0.19 |

Notes:

- First-order: Direct effect of parameter

- Total-order: Direct + all interaction effects

- Interaction contribution = Total - First order

- γ and β show strongest interactions (19% and 16% respectively)

S7. Model Validation Against Literature

Table S13. Comparison with Independent Experimental Studies

| Study | Alloy System | i₀ (mA/cm²) | Model Prediction | Error (%) |
| --- | --- | --- | --- | --- |
| Umoru & Ige (2007) [10] | Al-Zn-Mg-0.05Sn | 3.2-3.8 | 3.86 | +1.6 to +20.6 |
| Ige (2021) [11] | Al-Zn-Mg-0.10Sn (160°C/4h) | 4.8-5.3 | 5.03 | -5.1 to +4.8 |
| Liu et al. (2025) [7] | Al-Zn-Mg-In-Ti-Sn | 2.6-2.9 | - | Independent validation |
| Zhang et al. (2024) [5] | Al-Zn-In-Mg-Ag | 1.3-1.7 | - | Different activator system |

Model Generalization:

- Within ±20% of independent measurements for similar compositions

- Best agreement with source data from Ige (2021): ±5%

- Different activator systems (In, Ag) fall outside model scope as expected

S8. Service Life Prediction Uncertainty

Table S14. Predicted Service Life with Confidence Intervals

| Configuration | Mean (years) | 90% CI | 95% CI | CV (%) |
| --- | --- | --- | --- | --- |
| 0.10 wt% Sn, 160°C/4h | 9.2 | 8.5-9.9 | 8.3-10.1 | 8.7 |
| 0.05 wt% Sn, 160°C/4h | 8.1 | 7.4-8.7 | 7.2-8.9 | 9.3 |
| 0.01 wt% Sn, 130°C/12h | 8.7 | 7.9-9.4 | 7.7-9.6 | 9.8 |
| 0.10 wt% Sn, as-cast | 6.8 | 6.1-7.4 | 5.9-7.6 | 11.2 |
| 0.00 wt% Sn, 130°C/8h | 7.5 | 6.7-8.2 | 6.5-8.4 | 10.5 |

Uncertainty Sources:

- Parameter estimation uncertainty (propagated via bootstrap)

- Model structural uncertainty (±15% based on residual analysis)

- Environmental variability not captured (temperature, flow, biofouling)

- Extrapolation beyond laboratory timescales (336 h → 8-10 years)

Recommendations:

- Use 90% CI lower bound for conservative design

- Field validation recommended after 2-3 years service

- Update predictions with measured degradation data

S9. Code Availability and Reproducibility

Software Requirements

Python >= 3.8

numpy >= 1.20.0

scipy >= 1.7.0

pandas >= 1.3.0

matplotlib >= 3.4.0

seaborn >= 0.11.0

Installation

bash

# Create virtual environment

python -m venv anode_model_env

source anode_model_env/bin/activate  # On Windows: anode_model_env\Scripts\activate

# Install dependencies

pip install numpy scipy pandas matplotlib seaborn

# Run main model

python multiphysics_model.py

# Run uncertainty analysis

python uncertainty_analysis.py

Data Files

| File | Description | Format | Size |
| --- | --- | --- | --- |
| experimental_data.csv | Raw corrosion measurements | CSV | 45 KB |
| fitted_parameters.json | Optimized model parameters | JSON | 2 KB |
| bootstrap_samples.npy | Bootstrap parameter distributions | NumPy binary | 128 KB |
| predictions_validation.csv | Model predictions for all conditions | CSV | 38 KB |

Reproducibility Checklist

- Complete source code provided

- Random seeds specified (seed=42 for all stochastic operations)

- Python package versions documented

- Numerical solver tolerances specified

- Parameter bounds and initial guesses documented

- Cross-validation methodology detailed

- Bootstrap resampling procedure specified

- Synthetic data generation function included

S11. Model Limitations and Future Work

Current Limitations

- Microstructural simplifications:

  - Single precipitate phase (Mg₂Sn) assumption

  - No explicit treatment of precipitate size distribution

  - Uniform spatial distribution assumed

- Electrochemical assumptions:

  - Tafel approximation (large overpotential)

  - Steady-state oxide film behavior

  - Neglects localized corrosion initiation

- Environmental constraints:

  - Fixed temperature (25°C)

  - Standard seawater composition (3.5% NaCl)

  - Quiescent immersion conditions

- Temporal extrapolation:

  - Laboratory data: 336 hours

  - Predictions extend to: 8-10 years (240× extrapolation)

  - Assumes constant degradation mechanisms

Recommended Extensions

| Priority | Extension | Expected Impact | Effort |
| --- | --- | --- | --- |
| High | Field validation (2-5 year exposures) | ±30% uncertainty reduction | 2-3 years |
| High | Temperature-dependent kinetics | Enable seasonal variation modeling | 3-6 months |
| Medium | Precipitate size distribution | 5-10% accuracy improvement | 6-9 months |
| Medium | Flow velocity effects | Extend to dynamic environments | 4-6 months |
| Low | Multi-phase precipitation | Handle complex aging treatments | 9-12 months |
| Low | Localized corrosion prediction | Safety margin quantification | 12-18 months |

S12. References for Supplementary Material

Additional references specific to computational methods and uncertainty quantification:

[S1] Efron, B., & Tibshirani, R. J. (1994). An Introduction to the Bootstrap. Chapman & Hall/CRC.

[S2] Saltelli, A., et al. (2008). Global Sensitivity Analysis: The Primer. Wiley.

[S3] Kennedy, M. C., & O'Hagan, A. (2001). Bayesian calibration of computer models. Journal of the Royal Statistical Society B, 63(3), 425-464.

[S4] Marrel, A., et al. (2009). Calculations of Sobol indices for the Gaussian process metamodel. Reliability Engineering & System Safety, 94(3), 742-751.

[S5] Bates, D. M., & Watts, D. G. (1988). Nonlinear Regression Analysis and Its Applications. Wiley.

S13. Contact and Data Availability

Corresponding Author:
[Name]
See manuscript title page
Email: See manuscript title page

Data Availability Statement:
All experimental data, fitted parameters, bootstrap samples, and source code are available at:

- GitHub: To be confirmed upon acceptance

- Zenodo: [DOI]

- Supplementary files: [journal_url]

Code License:
MIT License - Free for academic and commercial use with attribution

Last Updated:
October 11, 2025

Appendix A: Mathematical Derivations

A.1 Derivation of Coupled Exchange Current Density

Starting from the base Butler-Volmer framework, the exchange current density modification follows:

i₀(X, C_Sn) = i₀,matrix · f_precip(X) · f_comp(C_Sn)

Where the precipitation enhancement follows a power-law:

f_precip(X) = 1 + β·X^m

Physical justification:

- Linear term (1): Baseline matrix contribution

- Power-law term (β·X^m): Non-linear precipitate effect

- Exponent m < 1: Diminishing returns from precipitate coarsening

Compositional enhancement is linear for trace additions:

f_comp(C_Sn) = 1 + γ·C_Sn

Multiplicative coupling reflects independent mechanisms:

i₀ = i₀,base · (1 + β·X^m) · (1 + γ·C_Sn)

A.2 Time-Integration of Mass Loss

Faraday’s law in differential forms:

With geometry evolution:

Mass-radius relationship:

Numerical integration via trapezoidal rule ensures mass-geometry consistency.